Effect of segregation of sp-impurities on surface and grain

boundary magnetism in ferromagnetic metals

Monika Vsianska1,2,3, Hana Vemolova2, Mojmir Sob1,3,2

1Central European Institute of Technology, CEITEC MU, Masaryk University, Brno, Czech Republic

2Masaryk University, Faculty of Science, Department of Chemistry, Brno, Czech Republic

3Institute of Physics of Materials, Academy of Sciences of the Czech Republic, Brno, Czech Republic

The macroscopic mechanical behaviour of polycrystalline metallic materials is largely determined by cohesion of the grain boundaries (GB) which is strongly affected by segregated impurities. Here we present a systematic ab initio study of segregation of 12 non-magnetic sp-impurities (Al, Si, P, S, Ga, Ge, As, Se, In, Sn, Sb and Te) at Σ5(210) grain boundary (GB) and (210) free surface (FS) in fcc ferromagnetic cobalt and nickel and analyze their effect on structure, magnetic and mechanical properties. We determine preferred segregation sites at the Σ5(210) GB for the sp-impurities studied, their segregation enthalpies and strengthening/embrittling energies with their decomposition into the chemical and mechanical components. We find interstitially segregated Si as a GB cohesion enhancer, substitutionally segregated Al and interstitially segregated P with none or minimum strengthening effect and interstitially segregated S, Ge, As, Se and substitutionally segregated Ga, In, Sn, Sb and Te as GB embrittlers. In nickel, most of the above impurities nearly kill or substantially reduce the magnetic moments at the FS and, when segregating interstitially (i.e. Si, P, S, Ge, As, Se), also at the GB so that they provide atomically thin magnetically dead layers which may be very desirable in spintronics. Reduction of magnetic moments at the Σ5(210) GB in fcc ferromagnetic cobalt is, in absolute values, very similar to that in nickel. However, as the magnetic moment in bulk cobalt is higher, we do not observe magnetically dead layers here. It turns out that by focused impurity segregation we can generate atomically thin magnetic layers with tailored magnetization, which can contribute to a new development of technologically important materials. Most of our results are theoretical predictions and we hope that they may motivate experimentalists to conduct new investigations in this field.